## Slide 1
Common Softwood Classifications and Grades
Classification and Grade | Description or Use
Finish or selects - Up to 1 1/2 in. thick, 2 in. or more wide; graded on basis of appearance | 
B & BTR | Nearly clear, with only minor defects; suitable for natural finish
C | More and larger defects than B & BTR but suitable for paint finish
D | A little lower in quality than C but still suitable for paint finish
Boards - Up to 1 1/2 in. thick, 2 in. or more wide; graded for suitability for use in construction | 
SEL MER or 1 | Used in housing and light construction for exposed paneling, shelving, etc.
CONST 2 | Used for subfloors, roof sheathing, etc.
STD 3 | Used about the same as CONST 2 grade but a little lower in quality
UTIL 4 | Combines usefulness and lower cost for general construction purposes
ECON 5 | Used for low-grade sheathing, crating, and bracing
Dimension - 2 to 5 in. thick, 2 in. or more wide | 
Structural light framing | 2 to 4 in. thick, 2 to 4 in. wide; for engineered use when higher strength is needed
Select structural (SEL STR) | Used where high strength, stiffness and good appearance are needed
No. 1 | Used about the same as SEL STR grade, but a little lower in quality
No. 2 | Recommended for most general construction uses
No. 3 | Used for general construction where appearance is not a factor
Light framing | 2 to 4 in. thick, 2 to 4 in. wide; provides good appearance where high strength and high appearance are not needed
Construction | Recommended and widely used for general framing purposes
Standard | About the same uses as construction grade, but a little lower in quality
Utility | Used for studding, blocking, plates, etc., where economy and good strength are desired
Economy | Suitable for crating, bracing, and temporary construction
Studs | 2 to 4 in. thick, 2 to 4 in. wide; only one grade for studs, which is suitable for all stud uses
Structural joints and planks | 2 to 4 in. thick, 6 in. and more wide; for engineering applications
Select structural | Used where high strength and stiffness and good appearance are needed
No. 1 | Used about the same as SEL STR grade, but a little lower quality
No. 2 | Recommended for most general construction use
No. 3 | For use in general construction where appearance is not a factor
Appearance and framing | 2 to 4 in. thick, 2 in. and more wide
A | Used in housing and light construction for high strength and finest appearance
Timbers - 5 in. or more in least dimension | 
Select structural | Used where superior strength and good appearance are needed
No. 1 | Similar to SEL STR grade, but a little lower in quality
No. 2 | Recommended for general construction
No. 3 | Used for rough general construction
Adapted from Structures and Environmental Handbook, Midwest Plan Service

## Slide 2
Sample Plywood Grade Stamps
Adapted from Structures and Environmental Handbook, Midwest Plan Service

## Slide 3
Veneer Grades
Source: Agricultural Structures. Instructional Materials Laboratory, University of Missouri-Columbia, 1999.

## Slide 4
Dimensions of Steel Stock